CS Hyde Company 1351 N. Milwaukee Ave., Lake Villa, IL 60046 Ph. 847-395-0325 Fax 847-395-0334 sales@cshyde.com. PRODUCT INFORMATION

19-__A UHMW Film w/ Acrylic Adhesive

PRODUCT DESCRIPTION

UHMW is a super tough, abrasion resistant material. It has a high-slip/ non-stick surface similar to that of Teflon® but UHMW can take eight times the abrasion than that of Teflon® coated fiberglass and it is also very cost efficient. The UHMW film provides an excellent low friction, non-stick surface, in many ways similar to PTFE. The 19-A series is pressure sensitive with an aggressive permanent acrylic adhesive

APPLICATION INFORMATION

The 19-A series is used primarily in mechanical applications such as chute liners, wear pads, and guide rails. It can also be used in such applications as a glide surface for computer mouse. The acrylic transfer adhesive has a temperature range of 225ºF – 300ºF. Excellent UV, temperature, moisture and chemical resistance. Very versatile.

TECHNICAL DATA

Test Method; 19-3A; 19-5A; 19-10A; 19-20A. Backing Thickness (in.); .003; .005; .010; .020. Adhesive Thickness (in.); .002. Adhesion; Acrylic. Elongation (%); ASTM-D 882; 300. Tensile Strength (psi); ASTM-D 882; 6000. Dielectric Strength (V/mil); ASTM-D 149; 3000. Thermal Conductivity; (73)[(BTUin)/(ft²hrºF)]; 0.44. Temperature Range (cont.); 0ºF to 200ºF. Water Absorption; .01. Density (g/cc); .93. Heat Distortion (ºF); ISO R75 Method A; 203. Coefficient of Thermal Expansion; ~1.1x104. Deformation (%); 2000 psi, 6hr.,122ºF; 6-8. Dissipation Factor; ASTM-D 150; 0.0004.

Width:		25” up to 24”

Length:          18 (or) 36 yards