This film offers high heat resistance coupled with high strength, stiffness, UV stability and broad chemical resistance.  The combination of outstanding thermal, mechanical and electrical properties together with exceptional flame resistance and thermoform-ability, provide unprecedented performance for a wide variety of demanding new design concepts.

The following physical property information is based on typical values of the base Ultem® 1000 resin as well as test results obtained from actual film testing.

| ELECTRICAL Properties | Test Method | Result Metric English |  |
| --- | --- | --- | --- |
| Surface Resistivity | ASTM D257 | >1016 Ohms | >1016 Ohms |
| Dielectric Strength at 0.003 | ASTM D149 | 120 V/µm | 3050 V/mil |
| Dielectric Constant | ASTM D150 | 3.15 1 kHz | 3.15 1 kHz |
| Dissipation Factor | ASTM D150 | 0.0013 10 kHz | 0.0013 10 kHz |
| MECHANICAL Properties | Test Method | Result Metric English |  |
| Tensile Strength at yield | ASTM D882 | 98 MPa | 14.2 kpsi |
| Elongation at break | ASTM D882 | 52 % | 52 % |
| Tensile Modulus | ASTM D882 | 3275 MPa | 475 kpsi |
| Flexural Modulus | ASTM D790 | 331 MPa | 48 kpsi |
| Tear Strength – prop. | ASTM D1004 |  | 381 g/mil |
| OTHER Properties | Test Method | Result Metric English |  |
| Specific Gravity | ASTM D792 | 1.27 | 1.27 |
| Water Absorption at 24 hours | ASTM D570 | 0.25 % | 0.25 % |
| Refractive Index | - | 1.658 | 1.658 |
| Haze | ASTM D1003 | % | % |
| Area Factor | - |  | 21888 in²/lb/mil |
| THERMAL Properties | Test Method | Result Metric English |  |
| Continuous Use Temp. -UL | - | 170 ºC | 338 ºF |
| Heat Deflection Temp. at 264 psi | ASTM D648 | 201 ºC | 394 ºF |
| Melt Temp – DSC | - | ºC | ºF |
| Glass Transition Temp. | ASTM D3418 | 216 ºC | 420 ºF |
| UL Rating – UL94 | - | VTM-0 | VTM-0 |
| L.O.I. | ASTM D2862 | 27 % | 27% |
| NBS Smoke | ASTM E662 | 6 DMax | 6 DMax |