# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046

## PRODUCT INFORMATION

73-CCF Series

Light Density Sponge /

###### Closed Cell

###### Silicone Foam

Product Description:

# This unique product offers a compression deflection of a medium density sponge but has the light density of open cell foam.  It combines the best of both worlds.  Silicone exhibits a wish list of characteristics including superb chemical resistance, high temperature performance, good thermal and electrical resistance, long-term resiliency, and easy fabrication.  It also possesses excellent UV and ozone resistance.  Silicone is odorless, tasteless and non-toxic.  Silicone foam is grey in color, lightweight and flexible with a smooth skin on both sides.

Common Applications:

# Silicone foam can be used for insulating and cushioning electronic assemblies.  It can also be used for gaskets, seals, air filters, thermal shielding, cushioning for aviation, automotive and locomotive industries as well as flame-retardant applications.  Silicone foam is also approved for repeated food contact.

### TYPICAL PROPERTIES

| Property | Test Method | Silicone Foam |
| --- | --- | --- |
| Density | ASTM D3574 | 20-25 pcf |
| Compression Deflection | ASTM D1056 | 8-12 psi |
| Compression Set | ASTM D1056 | <10% |
| Tensile | ASTM D412 | 50-75 psi |
| Elongation | ASTM D412 | Min 80% |
| Bend Fatigue | 24 hrs @ 300ºF | Pass |
| Temperature Range °F (static) | SAE J2236 | -67 to +392 |
| Vertical Flammability | FAR 25.853 | Pass |
| Flame Resistance | UL 94 | V-0 |
| Thermal Conductivity | ASATM C-518 | .09 W/m K |
| Water Absorption | ASTM D570 | 1.5% |

Available Industry Specifications:

*UL 94 V-0

*AMS3195

*FDA APPROVED INGREDIENTS