# CS Hyde Company

    - FAX: 800-441-8063 		  PRODUCT INFORMATION

1351 North Milwaukee Avenue

19-HB  Series

UHMW Polyethylene Film with 3M 9482PC High Bond Adhesive

# Lake Villa, IL  60046

## Product # 	19-___HB

Product Description:

UHMW is a super tough, abrasion resistant material.  It has a high-slip/ non-stick surface similar to that of Teflon® but UHMW can take eight times the abrasion than that of Teflon® coated fiberglass and it is also very cost efficient.  The UHMW film provides an excellent low friction, non-stick surface, in many ways similar to PTFE.  The 3M 9482PC High Bond adhesive has outstanding temperature and chemical resistance.  The bond strength actually increases over time and temperature.  High humidity has a minimal effect on adhesive performance.  This material is extremely water resistant as well; after 100 hours in room temperature water the bond actually shows an increase in strength.

Performance & Application Information:

The 19-HB series is used primarily in mechanical applications such as chute liners, wear pads, and guide rails.  It can also be used in such applications as a glide surface for computer mouse.  This particular product has a modified adhesive system which is a good choice for applications which require adhesive to Low Surface Energy plastics, powder coatings and oily metals.

### TYPICAL PROPERTIES

|  | 19-10HB | 19-20HB | 19-30HB |
| --- | --- | --- | --- |
| UHMW Thickness (in.) | .010 | .020 | .030 |
| High Tack Acrylic Adhesive (in.) | .002 | .002 | .002 |
| Adhesion (oz./in.) to stainless Steel | 80 | 80 | 80 |
| Elongation (%) | 300 | 300 | 300 |
| Dielectric Strength Volts | 9000 | 15000 | 30000 |
| Temperature Range | 0ºF to 180ºF |  |  |

Note:  The above are “typical values” which have a nominal range about them and are not intended for specification purposes.  Teflon® is a registered trademark of DuPont.